## Slide 1
Patching Steel to Rehabilitate Structures
Lesson and Project Overview
Notes: Patching Steel to Rehabilitate Structures Presentation, Repairing Cracked Steel Structures with Carbon Fiber Patches lesson, TeachEngineering.org
Detail of temporary repairs on steel structure of the Pawtucket River Bridge (1958); the bridge has since been replaced.
Image source: 2010 Marcbela (Marc N. Belanger), Wikimedia Commons https://commons.wikimedia.org/wiki/File:Pawtucket_bridge_detail-1.JPG

## Slide 2
Who is this?
Why is he so powerful and indestructible?
Is steel really indestructible?
If Superman were not the man of steel, what other material—stronger than steel— might he be made of? Must this new material be a metal?
Notes: Use animation to reveal pre-assessment questions to lead a class discussion about strong materials.
What is stronger than steel?
Image source: 2007 Gareth Simpson, Flickr (CC BY 2.0) https://www.flickr.com/photos/xurble/376591423 and CC license: https://creativecommons.org/licenses/by/2.0/legalcode

## Slide 3
The Problem
Notes: Fatigue cracking in a bridge girder starting from weld defects at a weld intersection point.
While in slide show mode, click on bottom right inset image to go to MDPI research paper web page: “Fatigue-Prone Details in Steel Bridges” by Reza Haghani in Buildings at http://www.mdpi.com/2075-5309/2/4/456/htm
Image source: MDPI. Used with permission. http://www.mdpi.com/2075-5309/2/4/456/htm

## Slide 4
I-35W Mississippi River Bridge collapse
Minneapolis, MN, August 1, 2007
Notes: The bridge before/intact and then the scene at the I-35W Mississippi River Bridge the first morning after its collapse.
This eight-lane steel truss arch bridge suddenly collapsed during the evening rush hour, killing 13 people and injuring 145 others. A design flaw is the likely cause—a too-thin gusset plate ripped along a line of rivets, plus the additional weight on the bridge at the time of the collapse contributed to the catastrophic failure. (text source: https://en.wikipedia.org/wiki/I-35W_Mississippi_River_bridge)
While in slide show mode, click the 3 camera icons to open the following 3 videos:
(left) When a Bridge Falls: Disaster in Minneapolis | Retro Report | The New York Times (9:56 minutes) https://www.youtube.com/watch?v=74JNl5n-YdI
(middle) Seconds after Minneapolis Bridge Collapse! (1:56 minutes) https://www.youtube.com/watch?v=5euNMj9oEZs
(right) I35-W bridge collapse (actual footage) (39 seconds) https://www.youtube.com/watch?v=z1uscpZt8EQ
Image sources:
Intact bridge: 2006 Elkman, Wikimedia Commons https://commons.wikimedia.org/wiki/File:I-35W_Bridge_2.jpg
Collapsed bridge: 2007 Mike Wills, Flickr via Wikimedia Commons https://commons.wikimedia.org/wiki/File:I35_Bridge_Collapse_4crop.jpg

## Slide 5
Alexander Kielland Platform
Norwegian North Sea | March 27, 1980
Notes: Description: On the first image, the platform on the right is a semi-submersible “flotel”—which is a floating hotel that housed offshore drilling workers in Norwegian waters in 1980. (Click for next image) That rig capsized when one of its five legs (columns) failed in severe winds, but not an extreme storm. The disaster killed 123 of the 212 people on the platform. One of its bracings failed due to material fatigue, initiating a succession of failures. The entire rig collapsed only 14 minutes after the first leg failed. It was later discovered that the weld that attached a sonar instrument to the bracing contained cracks, which had probably been their since fabrication and then worsened over time.
While in slide show mode, click the two small images to open the following online videos:
(top diagram) Alexander Kieland by luis282008 (2:39 minutes) https://www.youtube.com/watch?v=7QVn3NUW_aQ
(bottom photo) Alexander Kielland ulykken by Inger Mari (3:17 minutes) https://www.youtube.com/watch?v=fNI6_8JQXzQ
Image sources:
Intact platform (background image): 2009 Norsk Oljemuseum, Norwegian Petroleum Museum, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Alexander_L_Kielland_and_Edda_2-7C_NOMF-02663-1-650.jpg
Collapsed platform in storm waters: 1980 Jan A. Tjemsland (photographer), Norwegian Petroleum Museum, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Alexander_L_Kielland_Column_D_with_fractures_NOMF-02663-1-647.jpg
Collapsed column floats in water: 1980 Jan A. Tjemsland (photographer), Norwegian Petroleum Museum, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Alexander_L_Kielland_Column_D_drifting_in_the_water_NOMF-02697-1-172.jpg
Diagram showing location of original fatigue crack: 2009 Wiki-Chris, Wikipedia Commons https://commons.wikimedia.org/wiki/File:ALK_columns_fractures_norwegian.png
Photo of failed bracing/strut in a museum: 2007 Jarle Vines, Wikimedia Commons (CC BY-SA 3.0) https://commons.wikimedia.org/wiki/File:Kielland_ulykken.jpg https://creativecommons.org/licenses/by-sa/3.0/

## Slide 6: Once a crack is detected, is it possible to stop it from growing?
Fatigue cracks form in steel structures due to cyclic loads. These initiate at locations of stress concentrations such as notches, weld details and holes.
Under repeated loading, cracks propagate compromising the integrity of structure
The Engineering Challenge
Notes: While in slide show mode, click the small blue 2D drawing and rainbow part images to open the following online videos:
(blue drawing) Crack propagation, finite elements (8 seconds) https://www.youtube.com/watch?v=G5K_04I_XkE
(rainbow part) Crack propagation through grain boundary (10 seconds) https://www.youtube.com/watch?v=qMBtYq9vc78
Image sources:
Background photograph: A photo shows fatigue cracking in the riveted connection of cross-bracing elements: Figure 13 in “Fatigue-Prone Details in Steel Bridges” by Reza Haghani, Mohammad Al-Emrani and Mohsen Heshmati in Buildings, Vol. 2, Issue 2 via MDPI. Used with permission. Courtesy of Dr. John W. Fisher, Lehigh University. http://www.mdpi.com/2075-5309/2/4/456/htm
Blue 2D FEM drawing of cylindrically shaped magnetic shield: 2007 Zureks, Wikimedia Commons https://commons.wikimedia.org/wiki/File:FEM_example_of_2D_solution.png
Rainbow part simulation of FEA deformation: 2008 Tryphont, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Displacements.JPG

## Slide 7: Traditional Methods to Repair Cracked Steel
Crack Stop Holes
Difficult to drill in reduced places
Holes may compromise structure strength
Notes: While in slide show mode, click the small bluish image to open the following online video:
Cracking with Holes (20 seconds) https://www.youtube.com/watch?v=03tQhVDHbQs
Image sources:
Drawing of cracked beam & end holes: Maritime; no usage restrictions for non-commercial educational purposes; http://www.maritime.org/doc/dc/part8.htm
Video (blue image): Cracking with Holes (20 seconds) https://www.youtube.com/watch?v=03tQhVDHbQs

## Slide 8: Traditional Methods to Repair Cracked Steel
Difficult to drill and collocate in reduced places
Difficult near bolts and angles
Induces stress concentrations
Cover Plates
Lesson and Project Overview
Notes: An illustrated of a bolted doubler plate repair. Dashed line represents crack beneath doubler plate and circle is the hole drilled to remove the crack tip.
Image source: 2013 Manual for Repair and Retrofit of Fatigue Cracks in Steel Bridges, FHWA publication no. FHWA-IF-13-020 (Figure 26, page 49)
http://www.fhwa.dot.gov/bridge/steel/pubs/hif13020/hif13020.pdf

## Slide 9: Traditional Methods to Repair Cracked Steel
Difficult to weld in reduced places
Risk of explosion
Induces stress concentrations
Repair Welding
Notes: A man welds a metal pipe.
Image source: 2006 Mgschuler, Wikimedia Commons https://upload.wikimedia.org/wikipedia/commons/9/97/SMAW.jpg

## Slide 10: Traditional Methods to Repair Cracked Steel
These techniques require the use of heavy equipment and produce irreversible modifications of the underlying structure
Notes: Image sources:
Rotary hammer drill for construction: 2008 KVDP, Wikimedia Commons https://commons.wikimedia.org/wiki/File:LargeDrill.jpg
Gas generator: 2010 Mgschuler, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Ranger_250_GXT_Front.jpg

## Slide 11: Better solutions?
Could you repair a crack in steel using something like a band-aid?
Notes: Image sources:
Cracked lightning rod ball assembly: 2013 William Waterway, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Gay_Head_Light_-_with_Ben_Franklin_lightning_rod.jpg
Band-aid: 2014 Eloy, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Ap%C3%B3sito_adhesivo.svg

## Slide 12
A Band-Aid is a composite
Material made from two or more constituent materials with significantly different physical or chemical properties that, when combined, produce a material with characteristics different from the individual components
Initial question: Why does a Band-Aid work?
stronger material + stronger adhesive?
protective strip
adhesive
pad + antibiotic
Notes: Image source: (Band-Aid) 2006 W0lfie, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Band-Aid_close-up.jpg

## Slide 13
stronger material + stronger adhesive?
Notes: Image sources:
Truck camper: Melanie van Zyl, used with permission; 10 reasons to travel with Gorilla Duct Tape http://www.getaway.co.za/gear-reviews/10-gorilla-duct-tape/
Duct tape layers diagram: 2016 Miguel R. Ramirez (author), Mathematics Dept. Galena Park High School and University of Houston RET
Gorilla tape roll: 2012 ratha, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Gorilla_tape_-_01.jpg

## Slide 14
Composites
Lesson and Project Overview
Notes: While in slide show mode, click on the four smaller images to open the following online videos:
(plane) Composites in Aviation by BioNetwork (6:37 minutes) https://www.youtube.com/watch?v=wXxn-8OA8Ac
(tire) Intro to Composites by BioNetwork (4:12 minutes) https://www.youtube.com/watch?v=WYqCnEvTRUQ
(bridge) 5 Steps of the Pultrusion Process (2:05 minutes) https://www.youtube.com/watch?v=1sH9rIGWNvc
(watch) Graphene: Composite Materials (3:22 minutes) https://www.youtube.com/watch?v=LTa_ileMJxE
Image sources:
Plane/bomber: 2008 U.S. Air Force, Wikimedia Commons https://commons.wikimedia.org/wiki/File:US_Air_Force_B-2_Spirit.jpg
Airless radial tire: 2012 TweelTech, Wikimedia Commons https://commons.wikimedia.org/wiki/File:MICHELIN_X_Tweel_SSL.JPG
Blue ped bridge: 2001 Pontis21, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Lleida_GFRP_Pedestrian_bridge.jpg
Watch: 2010 Dave P, Flickr https://www.flickr.com/photos/34148992@N07/4276953256 (non-commercial use)

## Slide 15
Epoxy Adhesives
Lesson and Project Overview
Notes: While in slide show mode, click on the four smaller images to open the following online videos:
(clear drop) 3M’s Tough Stuff vs. 3/8 Rivet Shear Test (31 seconds) https://www.youtube.com/watch?v=4kHflHJEfAM
(brush) Physical Strength Propereties of Epoxy Adhesives (2:57 minutes) https://www.youtube.com/watch?v=4WhBvSk8ajA
(2 bottles) Fabrico, a Division of EIS – High Strength Adhesives (4:26 minutes) https://www.youtube.com/watch?v=MKIlireFOIQ
(gray caulk) 3M’s Tough Stuff vs. Spot Weld Impact Test (32 seconds) https://www.youtube.com/watch?v=CPR28olqf5Y
Image sources:
Clear adhesive drop: 2006 Babi Hijau, Wikimedia Commons https://commons.wikimedia.org/wiki/File:AdhesivesForHouseUse004.jpg
Brush liquid glue: 2008 Simon Eugster, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Animal_glue_liquid.jpg
Epoxy 2 bottles: 2012 Simon A. Eugster, Wikimedia Commons https://commons.wikimedia.org/wiki/File:2K_Adhesive_Z-Poxy.jpg
Gray silicone caulking: 2007 Achim Hering, Wikipedia Commons https://commons.wikimedia.org/wiki/File:Caulking.jpg

## Slide 16
Carbon-Fiber-Reinforced Polymers (CFRP)
Notes: While in slide show mode, click on the two smaller images to open the following online videos:
(fabric with blue tape) Carbon Fiber by Maddbluntz (camera zooms in from a bicycle part to the highest possible visual magnification of carbon fiber) (3:17 minutes) https://www.youtube.com/watch?v=q0mQk1s4tKo
(carbon fiber weave) Rhino Carbon Fiber Shear Pin Strength Test (3:05 minutes) https://www.youtube.com/watch?feature=trueview-instream&v=vgH8eyCN8MI
Image sources:
Black woven fabric with blue tape (carbon fiber): 2005 Hadhuey, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Kohlenstofffasermatte.jpg
Carbon fiber weave: 2010 PandamicPhoto.com, Flickr (CC BY-SA 2.0) https://www.flickr.com/photos/poppingseed/4437414360

## Slide 17
CFRP-Epoxy Adhesive Composites
Notes: While in slide show mode, click on the six smaller images to open the following online videos and website:
(yellow-suited man) Concrete Bridge Repair w Fiber Reinforced Polymers – Carbon Wrap Solutions (shows three bridge repair examples) (4:32 minutes) https://www.youtube.com/watch?v=NSbpl9f0lO8
(runners on track) Oscar Pistorius runs 400M London Summer Olympics 2012 (4:50 minutes; start at 2 minutes in) https://www.youtube.com/watch?v=vB_g-RSIGfM
(artificial legs) High-Tech Running Prosthetics (2:05 minutes) https://www.youtube.com/watch?v=P27GVE6n8lU
(BMW car frame) Steel Shaft vs. Carbon Fiber Shaft (5:31 minutes) https://www.youtube.com/watch?v=hjErH4_1fks
(car bumper honeycomb) Getting to Know Fiber Reinforced Polymers (7:27 minutes) https://www.youtube.com/watch?v=iqD9hBQXi5Y
In addition, click on http://www.imasengiken.co.jp/en/lapoc/sport.html to see various prosthetic products made by Imasen Engineering Corporation
Images sources:
Yellow-suited man and black patch (dry fabric placed on saturated concrete): SilkaWrap Composites Fabrics brochure (pdf); used with permission; http://usa.sika.com/en/repair-protection/repair-protection-home/Documents_Refurbishment/Brochures_RP.html?page=2
Runners on track: 2012 Darren Wilkinson, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Mens_400m_semi_final_2_-_Oscar_Pistorius_Nigel_Levine.jpg
Artificial legs/feet: 2011 Nick Webb, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Oscar_Pistorius_at_International_Paralympic_Day,_Trafalgar_Square,_London_-_20110908.jpg
BMW i3 car chassis: 2013 MotorBlog, Wikimedia Commons https://commons.wikimedia.org/wiki/File:IAA_2013_BMW_i3_(9833675545).jpg
Car bumper honeycomb structure: 2013 youkeys, Wikimedia Commons https://upload.wikimedia.org/wikipedia/commons/4/49/2013_IAA_BMW_i3_Honeycomb_structure.jpg

## Slide 18: Fiber Reinforced Polymers
Composite material made of a polymer matrix reinforced with fibers
The polymer is usually an epoxy, vinylester or polyester thermosetting plastic
Fibers are usually glass, carbon or aramid; paper, wood or asbestos may be used
The alignment and weave of the cloth fibers is designed to optimize the strength and stiffness properties of the resulting material

## Slide 19: Carbon-Fiber-Reinforced Polymers
To create CFRP parts, sheets of carbon fiber cloth are layered into a mold in the shape of the final product.
Then the mold is filled with epoxy resin and heated or air-cured
The resulting part is very corrosion-resistant, stiff, with high fatigue strength, and strong for its weight

## Slide 20: CFRP Patches
Do not require welding or bolting
Do not modify underlying structure
Do not corrode
Do not add load to structure
Bonded to structure with structural adhesive
Reduces the strength range near the crack tip
Can be prestresed to provide compressive stress near the crack tip
Notes: Background images source:
Phares, B.M., Wipf, T.J., Klaiber, F.W., Abu-Hawash, A., and Lee, Y.S., Strengthening of Steel Girder Bridges Using FRP. (Figure 2b on page 4.) Proceedings, 2003 Mid-Continent Transportation Research Symposium, Ames IA, August. http://www.intrans.iastate.edu/publications/_documents/midcon-presentations/2003/pharesfrp.pdf. Used with permission granted by Dr. Lee.

## Slide 21
CFRP Patches to Rehabilitate Steel Structures
Engineering fact: Pre-stressed patches halt crack propagation
Lesson and Project Overview
Notes: While in slide show mode, click on the image to open the following online video: Sika CarboDur – Carbon fiber laminate for structural strengthening (2:09 minutes) https://www.youtube.com/watch?v=_oSGDt_XGHY
Image source:
Phares, B.M., Wipf, T.J., Klaiber, F.W., Abu-Hawash, A., and Lee, Y.S., Strengthening of Steel Girder Bridges Using FRP. (Figure 2b on page 4.) Proceedings, 2003 Mid-Continent Transportation Research Symposium, Ames IA, August. http://www.intrans.iastate.edu/publications/_documents/midcon-presentations/2003/pharesfrp.pdf. Used with permission granted by Dr. Lee.

## Slide 22
CFRP Patches to Rehabilitate Steel Structures
Pre-stressing equipment is bulky and impractical in many situations
Is there an alternative to stress the CFPR patches?
Lesson and Project Overview
Notes: Images source:
B/w photo shows a stress jack applying prestressing force: 2007 Anna Björklund and Joakim Höglind, master’s thesis, “Strengthening of steel structures with bonded prestressed laminates” at Chalmers University of Technology, Sweden (Figure 3.11a on page 27) http://publications.lib.chalmers.se/records/fulltext/63902.pdf
Man pulls long handle of anchorage assembly, and man under green bridge applies force: Phares, B.M., Wipf, T.J., Klaiber, F.W., Abu-Hawash, A., and Lee, Y.S., Strengthening of Steel Girder Bridges Using FRP. (Figures 2a and 2c on page 4.) Proceedings, 2003 Mid-Continent Transportation Research Symposium, Ames IA, August. http://www.intrans.iastate.edu/publications/_documents/midcon-presentations/2003/pharesfrp.pdf Used with permission granted by Dr. Lee.

## Slide 23
Shape Memory Alloys— Nitinol
Example applications
Notes: While in slide show mode, click on the five smaller images to open the following online videos:
(angioplasty-stent) 3D Animation of Coronary Stent Procedure (1:14 minutes) https://www.youtube.com/watch?v=t-zCBKRg7Cs
(roll of solder) Powerful Nitinol engine running on hot water (5:10 minutes) https://www.youtube.com/watch?v=YsOSqwrBb1I
(eyeglasses) SpaceMETA present NITINOL explanation by MIT (memory shape materials) (5:01 minutes) https://www.youtube.com/watch?v=2YVwpBAiA1A
(nitinol wires) Nitinol – Metallic Muscles with Shape Memory (watch deformed wire objects return to original shape when heated) (4:23 minutes) https://www.youtube.com/watch?v=-K57cbOhA5g
(dental braces on teeth) Nitanium Palatal Expander2 Multi-Purpose Finishing Appliance (43 seconds) https://www.youtube.com/watch?v=dqbzmKIUmuk
(dental braces off teeth) Nickle Titanium-NiTi-Orthodontic Wire (45 seconds) https://www.youtube.com/watch?v=cArEU2hLSFU
Image sources:
Angioplasty-balloon inflated w stent: 2016 BruceBlaus, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Angioplasty_-_Balloon_Inflated_with_Stent.png
Roll of solder: 2011 Bernd Rieke, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Weichlot.jpg
Eyeglasses: 2006 Wapcaplet, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Eyeglasses.jpg
Nitinol wires: 2011 Petermaerki, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Nitinol_draht.jpg
Dental braces on teeth: 2012 Jlhopgood, Flickr (CC BY-NC-SA 2.0) https://www.flickr.com/photos/jlhopgood/8023813025
Dental braces off teeth: 2011 Vinne2 and Sputnikcccp, Wikimedia Commons https://commons.wikimedia.org/wiki/File:Dental_braces.jpg

## Slide 24
Could nitinol be used to pre-stress CFRP-epoxy adhesive composite patches?
Shape Memory Alloys—Nitinol
Notes: While in slide show mode, click on the image to open a website about a professor who is developing a patch for repairing cracked steel: https://www.egr.uh.edu/news/201103/professor-developing-patch-repairing-cracked-steel
Image source:
2011 Nisal Abheetha Peiris (dissertation) U of Kentucky (Figure 5.20 on page 148: Placing laminate on the top flange) Used with permission. http://uknowledge.uky.edu/cgi/viewcontent.cgi?article=1207&amp;context=gradschool_diss

## Slide 25
A NiTiNb-CFRP patch is simple to pre-stress and apply, but…
NiTiNb-CFRP Patches to Rehabilitate Steel Structures
how effective is it?
Notes: Image sources:
NiTiNb-CFRP patches on steel: (2 photos) 2015 Structural Research Laboratory, Civil and Environmental Engineering Department, South Annex, University of Houston; used with permission

## Slide 26: List of embedded video and web page link in slides
Slide 3: While in slide show mode, click on bottom right inset image to go to MDPI image source web page: “Fatigue-Prone Details in Steel Bridges” by Reza Haghani in Buildings at http://www.mdpi.com/2075-5309/2/4/456/htm
Slide 4: While in slide show mode, click the three camera icons to open the following three videos:
(left) When a Bridge Falls: Disaster in Minneapolis | Retro Report | The New York Times (9:56 minutes) https://www.youtube.com/watch?v=74JNl5n-YdI
(middle) Seconds after Minneapolis Bridge Collapse! (1:56 minutes) https://www.youtube.com/watch?v=5euNMj9oEZs
(right) I35-W bridge collapse (actual footage) (39 seconds) https://www.youtube.com/watch?v=z1uscpZt8EQ
Slide 5: While in slide show mode, click the two small images to open the following online videos:
(top diagram) Alexander Kieland by luis282008 (2:39 minutes) https://www.youtube.com/watch?v=7QVn3NUW_aQ
(bottom photo) Alexander Kielland ulykken by Inger Mari (3:17 minutes) https://www.youtube.com/watch?v=fNI6_8JQXzQ
Slide 6: While in slide show mode, click the small blue 2D drawing and rainbow part images to open the following online videos:
(blue drawing) Crack propagation, finite elements (8 seconds) https://www.youtube.com/watch?v=G5K_04I_XkE
(rainbow part) Crack propagation through grain boundary (10 seconds) https://www.youtube.com/watch?v=qMBtYq9vc78
Slide 7: While in slide show mode, click the small bluish image to open the following online video: Cracking with Holes (20 seconds) https://www.youtube.com/watch?v=03tQhVDHbQs
Slide 14: While in slide show mode, click on the four smaller images to open the following online videos:
(plane) Composites in Aviation by BioNetwork (6:37 minutes) https://www.youtube.com/watch?v=wXxn-8OA8Ac
(tire) Intro to Composites by BioNetwork (4:12 minutes) https://www.youtube.com/watch?v=WYqCnEvTRUQ
(bridge) 5 Steps of the Pultrusion Process (2:05 minutes) https://www.youtube.com/watch?v=1sH9rIGWNvc
(watch) Graphene: Composite Materials (3:22 minutes) https://www.youtube.com/watch?v=LTa_ileMJxE
Slide 15: While in slide show mode, click on the four smaller images to open the following online videos:
(clear drop) 3M’s Tough Stuff vs. 3/8 Rivet Shear Test (31 seconds) https://www.youtube.com/watch?v=4kHflHJEfAM
(brush) Physical Strength Propereties of Epoxy Adhesives (2:57 minutes) https://www.youtube.com/watch?v=4WhBvSk8ajA
(2 bottles) Fabrico, a Division of EIS – High Strength Adhesives (4:26 minutes) https://www.youtube.com/watch?v=MKIlireFOIQ
(gray caulk) 3M’s Tough Stuff vs. Spot Weld Impact Test (32 seconds) https://www.youtube.com/watch?v=CPR28olqf5Y

## Slide 27: List of embedded video and web page link in slides (continued)
Slide 16: While in slide show mode, click on the two smaller images to open the following online videos:
(fabric with blue tape) Carbon Fiber by Maddbluntz (camera zooms in from a bicycle part to the highest possible visual magnification of carbon fiber) (3:17 minutes) https://www.youtube.com/watch?v=q0mQk1s4tKo
(carbon fiber weave) Rhino Carbon Fiber Shear Pin Strength Test (3:05 minutes) https://www.youtube.com/watch?feature=trueview-instream&v=vgH8eyCN8MI
Slide 17: While in slide show mode, click on the six smaller images to open the following online videos and website:
(yellow-suited man) Concrete Bridge Repair w Fiber Reinforced Polymers – Carbon Wrap Solutions (shows three bridge repair examples) (4:32 minutes) https://www.youtube.com/watch?v=NSbpl9f0lO8
(runners on track) Oscar Pistorius runs 400M London Summer Olympics 2012 (4:50 minutes; start at 2 minutes in) https://www.youtube.com/watch?v=vB_g-RSIGfM
(artificial legs) High-Tech Running Prosthetics (2:05 minutes) https://www.youtube.com/watch?v=P27GVE6n8lU
(BMW car frame) Steel Shaft vs. Carbon Fiber Shaft (5:31 minutes) https://www.youtube.com/watch?v=hjErH4_1fks
(car bumper honeycomb) Getting to Know Fiber Reinforced Polymers (7:27 minutes) https://www.youtube.com/watch?v=iqD9hBQXi5Y
(artificial leg) Imasen Engineering Corporation’s Lapoc System Prostheses web page showing various products http://www.imasengiken.co.jp/en/lapoc/sport.html
Slide 21: While in slide show mode, click on the image to open the following online video: Sika CarboDur – Carbon fiber laminate for structural strengthening (2:09 minutes) https://www.youtube.com/watch?v=_oSGDt_XGHY
Slide 23: While in slide show mode, click on the five smaller images to open the following online videos:
(angioplasty-stent) 3D Animation of Coronary Stent Procedure (1:14 minutes) https://www.youtube.com/watch?v=t-zCBKRg7Cs
(roll of solder) Powerful Nitinol engine running on hot water (5:10 minutes) https://www.youtube.com/watch?v=YsOSqwrBb1I
(eyeglasses) SpaceMETA present NITINOL explanation by MIT (memory shape materials) (5:01 minutes) https://www.youtube.com/watch?v=2YVwpBAiA1A
(nitinol wires) Nitinol – Metallic Muscles with Shape Memory (watch deformed wire objects return to original shape when heated) (4:23 minutes) https://www.youtube.com/watch?v=-K57cbOhA5g
(dental braces on teeth) Nitanium Palatal Expander2 Multi-Purpose Finishing Appliance (43 seconds) https://www.youtube.com/watch?v=dqbzmKIUmuk
(dental braces off teeth) Nickle Titanium-NiTi-Orthodontic Wire (45 seconds) https://www.youtube.com/watch?v=cArEU2hLSFU
Slide 24 – While in slide show mode, click on the image to open a website about a professor who is developing a patch for repairing cracked steel: https://www.egr.uh.edu/news/201103/professor-developing-patch-repairing-cracked-steel