## Slide 1: Lab Procedure for Standard/Control Sample Preparation
Notes: Lab Procedure for Standard/Control Sample Preparation, Lab Research to Engineer a Phosphorescent Bioplastic activity, TeachEngineering.org
///
All images: 2016 Jamie Sorrell, RET Program, School of Polymers and High Performance Materials, University of Southern Mississippi (author)

## Slide 2: Preheat a hot plate to 400°C
Notes: Walk students through this procedure, which matches their handouts

## Slide 3: Label tops and bottoms of petri dishes with group initials, sample name and reactant concentration

## Slide 4: In 1,000-ml beaker, add 10 g of cornstarch

## Slide 5: Using a 10-ml graduated cylinder, add 5 ml of vinegar to the same beaker

## Slide 6: Using a 10-ml graduated cylinder, add 5 ml of glycerin to the same beaker

## Slide 7: Using a 100-ml graduated cylinder, add 60 ml of water to the same beaker

## Slide 8: Use your measured water to get the glycerin residue from the graduated cylinder in the previous step

## Slide 9: Using a silicone spatula, stir until all material is completely dissolved

## Slide 10: Using a 100-ml graduated cylinder, measure out 60 ml of the mixture, and put into a clean 250-ml beaker

## Slide 11: Add 0.6 grams of phosphorescent powder to the 60-ml mixture in the 250-ml beaker—and stir

## Slide 12: On the preheated hot plate, heat the mixture in the 250-ml beaker
400 °C 

## Slide 13: Continuously stir while heating the mixture for 6 mins and 30 secs
Notes: ** BE CONSISTANT WITH TIME FOR ALL YOUR SAMPLES **

## Slide 14: After 6 mins and 30 secs, the mixture becomes clear and/or a viscous solid
Notes: ** BE CONSISTANT WITH TIME FOR ALL YOUR SAMPLES **

## Slide 15: Using the silicone spatula, transfer the heated mixture to a prepared petri dish
Let the phosphorescence bioplastic dry overnight
Notes: Using the silicone spatula, transfer the heated mixture into a small petri dish that is lined with aluminum foil and labeled with the sample name.